Course Content

| Module 1 | MODULE TITLE | FUNDAMENTALS OF HIGHWAY MATERIAL TESTING |
| --- | --- | --- |
| Lectures 6 | Tutorial 6 |
| Learning Outcomes: Ability to understand the role of highway material engineer Ability to Understand experimental errors, sampling and equipment calibration Ability to understand basic statistics Ability to interpret test results |
| Outline syllabus Role of a Civil Engineering Laboratory in Civil Engineering/ Role of Materials Testers in Civil Engineering/ Operations of a Civil Engineering Laboratory/ Basic knowledge of construction/ Types and handling of Laboratory apparatus/ Importance of correct set-up of apparatus/ Importance of calibration/ Laboratory safety practice/ Basic properties of soils, gravel, bitumen, asphalt, cement, concrete and aggregate/ Sampling theory/ Calculation of volumes, densities etc/ Basic Quality Assurance/ Record keeping/ Essentials of management/ Quality assurance and specifications/ Daily programming of testing/ Measurement methods/ Interpretation of test results/ Introduction to statistics |
| Assessment scheme: 100% Continuous Assessment [ assignment on presentation of test results including statistics and data analysis and results interpretation] |

| Module 2 | MODULE TITLE | SOIL TESTING |
| --- | --- | --- |
| Lectures 9 | Practical 18 |
| Learning Outcomes: Ability to understand the Basic Soil Mechanics principals Ability to understand the design parameters related to highway design Ability to perform soil testing related to highway construction |
| Outline syllabus Introduction to soil and rock mechanics/ Mass volume relationships/ Testing and classification of soils for highway construction/ Introduction to soil compaction/ Measurement of the strength of soil/ Selection of fill material and quality controlling of field soil compaction Lab Assignments Soil sampling/ Determination of the moisture content/ Determination of the particle size distribution of soil/ Determination of Atterberg Limits (LL, PL &PI)/ Determination of the linear shrinkage/ Determination of the moisture density relationship/ Determination of the CBR of treated and untreated materials / Determination of the UCS of treated materials/ Determination CBR by DCP test/ Determination of the field density by nuclear method/ Determination of the field density by sand replacement method/ Determination of the field density by core cutter method |
| Assessment scheme: 100% Continuous Assessment [ Assignment on basic soil mechanics, preparation of test reports] |

| Module 3 | MODULE TITLE | AGGREGATE AND CONCRETE TESTING |
| --- | --- | --- |
| Lectures 14hrs | Practicals 16.5 hrs |
| Learning Outcomes: Ability to understand the properties of cement, aggregate and concrete Ability to perform tests on cement, aggregate and concrete Ability to perform concrete mix design |
| Outline Syllabus Properties of cement and aggregates/ Concrete mix design/ Properties of fresh and hardened concrete Lab assignments Testing of cement for strength, setting time and soundness/ Determination of the aggregate crushing value/ Determination of the 10% fineness value/ Sieve analysis of fine and coarse aggregates / Determination of the flakiness index of coarse aggregate / Determination of ALD of coarse aggregate / Determination of the dry bulk density, apparent relative density and water absorption of fine and coarse aggregates/ Concrete mix design and testing of fresh and hardened concrete including flexural strength, splitting tensile strength and compressive strength |
| Assessment scheme: 100% Continuous Assessment [ Assignment on basic mix design calculation and preparation of test reports] |

| Module 4 | MODULE TITLE | BITUMIOUS MATERAIL TESTING |
| --- | --- | --- |
| Lectures 15 | Practical 18 |
| Learning Outcomes: Ability to understand the properties of bituminous material and hot mix asphalt Ability to perform bitumen and hot mix asphalt testing Ability to perform asphalt mix design |
| Outline syllabus Types of Bitumen / Properties of Bitumen/ Bitumen Classification/ Type of Surfacing/ Volumetric Properties of Hot Mix Asphalt/ Asphalt Mix Design Lab Assignment Determination of penetration value of bitumen / Determination of the softening point of bitumen / Determination of ductility of bitumen / Loss on heating of bitumen (Thin Film Oven Test )/ Viscosity of bituminous binders/ Determination of binder content / Determination of bulk relative density / Determination of the theoretical maximum relative density (Rice) / Determination of the void content / Determination of the stability and flow by means of Marshall method / Determination of the relative compaction of an asphalt mixture/ Determination of Binder Content by extraction and Ignite Method/ Tests on bituminous emulsions |
| Assessment scheme: 100% Continuous Assessment [ Assignment on asphalt mix design and preparation of test reports] |